1.Name：Magnesium Sulphate Anhydrous

2. Appearance: 80-100mesh White powder or 300mesh white powder or 20 mesh mini granular or 20 mesh extruded mini granular.

4.Content: 19.5% Mg or 19.8% Mg can be choosed.

5.Usage:

1./Cosmetics and Feeding : Bath salts ,exfoliants and skincare or animal feed additives.

2./Agriculture:

Fertilizer especially the liquid fertilizer to supply magnesium and sulfur for crops;corrects magnesium deficiency in soil.

3./Industry:

Tanning ,dyeing,papermaking,plastics,ceramics and fireproof materials.

| No. | Test Item | Specification |
| --- | --- | --- |
| 1 | Appearance | White powder |
| 2 | Purity | ≥98% |
| 3 | MgO | ≥32.6% |
| 4 | Mg | ≥19.5% |
| 5 | Fe(Iron) | ≤0.0030% |
| 6 | Cl(Chlorid) | 0.03%max |
| 7 | Pb(Heavy metal) | ≤0.002% |
| 8 | As(Arsenic) | ≤0.002% |
| 9 | S | 24%min |
| 10 | Water insoluble | ≤0.01% |
| 11 | PH(5%W/V solution) | 5-9 |

CAS ：7487-88-9‌

HS Code：2833210000

化学式：MgSO4