
CERTIFICATE OF ANALYSIS
	Product
	Calcium Chloride as flake

	Batch No.
	GR20201010
	Date of Report
	OCT 10TH, 2020

	Date of manufacture
	OCT 10TH, 2020
	Date of Expiry
	OCT 9TH, 2022

	Item
	Specification
	Test Result

	Description
	White or almost white crystalline flake

	CaCl2 Purity
	Based on CaCl2
	77% min
	77.69%

	Sodium Chloride
	Based on NaCl
	4.0% max
	2.15%

	Magnesium chloride 
	Based on MgCl2
	0.5% max
	0.20%

	Sulphate
	Based on SO42-
	0.05% max
	＜0.05%

	Heavy metals
	
	10ppm max
	＜10ppm

	Acid insoluble
	Gravimetry
	0.3% max
	＜0.3%

	Remarks:
	QUALIFIED



